## Slide 1
Legend
Blue: CATL 117Ah 3.7V batteries
Red: Heaters
Black: Insulation jackets to prevent heat propagation
Yellow: Thermocouples (T1 – T21)
C1
C2
C3
C4
C5
T1
T2
T3
T4
T5
T6
T7
T8
T9
T10
T11
T12
T13
T14
T15
T16
T17
T18
T19
T20
T21
Heater is placed directly on C2 without thermocouples between battery and heater. C2 is the trigger cell.
T1 and T21 are placed between the outer insulation jacket and air.
T2, T4, T10, T12, T14, T16, T18 and T20 are placed between insulation jacket and the battery cells.
T6 and T8 are in direct contact with the heater and insulation jacket.
T3, T7, T11, T15, T19 are placed on the safety vent of each battery cells.
T5, T9, T13 and T17 are placed between insulation jackets of each battery cells.